# Type: Solar Control Ultra-Clear Low-E Clear Insulating Glass

***“Solarban*®*”* 60 (2) “*Starphire*®*”* + *“Starphire”*** by Vitro Architectural Glass

**Outdoor Lite: *“Starphire”*** (ultra-clear) Float Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

**Indoor Lite: *“Starphire”*** (ultra-clear) Float Glass

**Low-E Coating: *“Solarban”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 74% | 0.29 | 0.27 | 0.41 | 0.48 | 11% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Ultra-Clear

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass