# Type: Solar Control Ultra-Clear Low-E Clear Insulating Glass

“Solarban®” 60 (2) “Starphire®” + “Starphire” by Vitro Architectural Glass

Outdoor Lite: “Starphire” (ultra-clear) Float Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

Indoor Lite: “Starphire” (ultra-clear) Float Glass

Low-E Coating: “Solarban” 60 Solar Control (Sputtered) by Vitro Architectural Glass

Location: Second Surface (2)

# Performance Values

| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| --- | --- | --- | --- | --- | --- |
| 74% | 0.29 | 0.27 | 0.41 | 0.48 | 11% |

Approved Manufacturers: Vitro Certified™ Fabricator Required

Certification: Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation Institute (www.c2ccertified.org).

Outdoor Appearance: Ultra-Clear

Insulating Unit Construction: 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass